## Slide 1: Growth and characterization of GaSb Quantum Rings for Intermediate Band Solar Cells
Cadiz PROMIS Workshop:18-20 May 2016
Work package 3: Materials for energy
D. Montesdeocaa, P. J. Carringtona, M. C. Wagenerb, J. R. Bothab, A. R. J.Marshalla, and A. Kriera
Lancaster University, UK.
Nelson Mandela Metropolitan University, SA.
Notes: Recently moved to UCL, but the bulk of the work was done whilst I was at Lancaster in collaboration with NMU and TEM done in Warwick.
And I’m going to talk about … specifically GaSb/GaAs QDs for SCs.

## Slide 2: Introduction
Radiation Transmitted
photon energy < band gap
Radiation Absorbed
photon energy > band gap
Transmission loss
Thermalized

## Slide 3: 3rd Generation Solar Cells
Third-generation cells utilise sub-band gap light.
Tandem/stacked cells have produced record efficiencies.
  Expensive and limited to concentrator systems.
Multi-junction PV cells
record = 46% (508x) 4-junction cell
Fraunhofer ISE

## Slide 4: Intermediate Band Solar Cell
The Solar Energy Institute in Madrid
Luque et al., Nature Photonics 6 (2012) 146
Luque and Marti, Phys. Rev. Lett. 78 (1997) 5014
Two operating principles of IBSC:
1) Voc Conservation
2) Two-Photon Subbandgap Photocurrent
3 Fermi levels( EF,C EF,V EF,IB)Partially filling of IB
- No overlapping of absorption
coefficient
- Partially filled IB

## Slide 5: Type II GaSb/GaAs QD/QR Solar Cell
GaAs control cell and 5 and 10 stacks of GaSb/GaAs QD/QR have been grown by Molecular Beam Epitaxy
MBE Veeco GEN xplor
SC Diameter 3.5mm

## Slide 6
dot density  1 x 1010 cm-2
QD/QR grown by self assembled in MBE (strain between GaAs and GaSb ≈7.8%)
QD/QR density 1010cm-2
QR formation: strain relief (No strain balanced layers required)
Type-II heterostructure  spatially indirect absorption/recombination
Type II GaSb/GaAs Quantum Rings

## Slide 7: Photo-response and IV under 1-sun
GaSb quantum rings extends the optical response up to 1400 nm
Short Circuit Current (Jsc) 27.9 mA/cm2 5.9% increase
Reduction on Open Circuit Voltage (Voc) ≈400meV
CB
VB
IB
VOC drop
AM 1.5

## Slide 8: Reason for VOC loss
Decrease in VOC due to thermal emission of holes quantum rings  competing optical and thermal hole-emission
  VOC recovered by cooling or by increasing optical intensity
Need to know/control the optical and thermal emission kinetics
    Absorption coefficient and hole emission rate
CB
VB
IB
optical transitions
thermal
H. fujita, J. James, Sem. Sci. Tech., 29 (2014) 035014
IB
thermal
optical
transitions

## Slide 9: Reason for VOC loss
Decrease in VOC due to thermal emission of holes quantum rings  competing optical and thermal hole-emission
  VOC recovered by cooling or by increasing optical intensity
Need to know/control the optical and thermal emission kinetics
    Absorption coefficient and hole emission rate
CB
VB
IB
optical transitions
thermal
H. fujita, J. James, Sem. Sci. Tech., 29 (2014) 035014
IB
Competing process
thermal
optical
transitions

## Slide 10: Two-photon response measurement
Conventional setup of photoresponse spectroscopy.
Sub-bandgap photoresponse limited by hole emission from quantum rings.
CB
VB
IB
primary
thermal

A
A
A

## Slide 11: Two-photon response measurement
Charging/photofilling the QR using a second excitation source counteracts hole emission
  Two-step excitation becomes discernable
CB
VB
IB
primary
secondary
B
trapping

A
A
A
B

## Slide 12: Two-photon response
GaSb quantum rings significantly extends photo-response
16 Kelvin
primary
thermal
CB
VB
QR
weak
PRIMARY
A

## Slide 13: Two-photon response
primary
thermal
CB
VB
QR
weak
PRIMARY +
PHOTOFILLING
16 Kelvin
A
+
B
B
A
A
Second, photofilling source enhances QR response
VERIFIES: 2-photon response via QR states
Wagener et al., Journal of Appl. Phys. 116 (2014) 044304

## Slide 14: Summary
Demonstrated quantum dot solar cell through incorporation of GaSb quantum rings in GaAs solar cell.
( 5 and 10 stacks od QD has been fabricated)
Extended cell operation well beyond GaAs response.
Increase in short circuit current about 5.9%.
Successfully demonstrated two-photon absorption using the type-II GaSb/GaAs system at low temperature.

## Slide 15: Acknowledgements
Dr. R. Beanland and Dr. Ana Sanchez (TEM) - University of Warwick
Dr Rob Airey and Dr. Ken Kennedy, (Processing) III-V National Centre, Sheffield
EU Marie-Curie photonics training network (PROMIS)
Thank you for your attention

## Slide 16: Solving the VOC loss
Open-circuit loss presently the central problem in quantum dot solar cell development
Need to reduce thermal emission from nanostructures
  Move quantum states deeper into band gap
  Increase effective barrier  avoid wetting layer formation
   incorporate barrier layers