## Slide 1
Nanometre Wide Avalanche Regions for High Performance SPADs: A review
Project members:
Salman Abdullah, ESR, EEE, Sheffield Prof. Chee Hing Tan, EEE, Sheffield Dr. Jo Shien Ng, EEE, Sheffield
PROMIS workshop Cadiz, 18th -20th May, 2016, Cadiz, Spain

## Slide 2: Device structure and field profile
Top contact
Top N-layer
Multiplication Charge sheet Grading Absorption Grading Bottom-P layer
Semi Insultaing-Substrate
E-field

## Slide 3: C-V measurement for APDs with high leakage
CV measurement for an InGaAs/AlGaAsSb SAMAPD
Higher leakage (Dark currents) do not permit accurate C measurement
5 10 15
Reverse bias [V]
0
20
25
Capacitance [F]
5.6e-12
5.8e-12
6.0e-12
6.2e-12
6.4e-12
6.6e-12
6.8e-12
7.0e-12
7.2e-12
7.4e-12
110um_1
110um_2
SF1082, NIPIP, R=110um
5 10 15
Reverse bias [V]
0
20
25
Phase angle [Degrees]
-90
-80
-70
-60
-50
-40
-30
-20
-10

## Slide 4: Z-F (three element model)technique for leaky devices
E. Andres et al., IEEE Trans. Elec. Device,
54(7), 2007
SF1082, R=110um, NIPIP
8000 10000 12000 14000 16000 18000
Real (Z)
0 2000 4000 6000
Imag (Z)
-10000
-8000
-6000
-4000
-2000
0
Exp. data 18.7V Exp. data 17.2V Exp. data 16.5V
Z-F fit, Rp=10536
Z-F fit, Rp=12821
Z-F fit, Rp=14487
SF1082, R=110um NIPIP
106
Test signal freq. [Hz]
104
105
107
108
Real (Z)
103
104
105
Exp.data, 18.7 V
Exp.data, 17.2 V
Exp.data, 16.5 V Z-F fit, C=8.6 pF Z-F fit, C=8.39 pF Z-F fit, C=8.52 pF

## Slide 5: Competing effects of PEB and avalanche multiplication
SF1082, R=110um
8 10 12
Reverse bias [V]
0
2
4
6
14
16
18
20
Current (Dark+Total) [A]
10-11
10-10
10-9
10-8
10-7
10-6
10-5
10-4
10-3
10-2
Responsivity (DC+AC) [A/W]
101
100
10-1
10-2
10-3
10-4
10-5
10-6
10-7
10
2
106
105
104
103
Id_110a Itotal_110a Id_110b Itotal_110b DC_Resp_110a AC_resp_110a DC_resp_110b AC_resp_110b

## Slide 6: Future plans
Device fabrication
  Surface treatment to avoid oxidation of AlGaAsSb layer
  Improve etching recipe e.g. to remove Al2O3
Characterization and assessment of devices

## Slide 7
Thank you for your attention!!