## Slide 1: Project 1.4: Hydrogenation of dilute nitrides for single photon emitters in photonic crystals
Saeed Younis

## Slide 2: Roadmap to Goal
The way we plan to achieve high intensity single-photon emitters working at 1.3 um:
  Obtain high-quality, uniform, N-containing QWs
    Emitting bellow 1 eV
    Can be hydrogenated
  Engineer the dot size and hydrogen dose to achieve the most suitable quantum confinement
    Single-peak PL at 1.3 um
  Integrate a PhC Cavity around the dot
    Yet better confinement through energy-locking of wandering dots
    Enhances the intensity through reduction of the spontaneous emission rate

## Slide 3: Effects of Hydrogenation on (In)GaAsN
For both GaAsN and InGaAsN, most effects are similar:
  Hydrogenation leads to blue-shifting of the peaks
    This is due to the passivation of N complexes
    Can lead to full recovery of the band gap energy to values of N-free material
    This effect is observed only when N is present in the material
  It also leads to reduction of PL intensity
    Luckily, hydrogenation is performed outside the dot
A. Polimeni et al., PRB 63, 201304 (2001).
M. Bissiri et al., PRB 65, 235210 (2002).

## Slide 4: GaAsN Quantum Dots
For sufficiently small mask sizes
  Quantum confinement achieved
    One single peak with < 150 uW FWHM
  Variation between identical dots is on the order of only ~10 meV !
    Their emission falls within ~40 meV
    BUT the starting uniformity of the QW was ~30 meV
S. Birindelli, M. Felici, et al., Nano Lett. 14, 1275 (2014).

## Slide 5: PhC Cavity in GaAsN
Courtesy of G. Pettinari, IFN-CNR
5 µm
500 nm
200 nm
Suspended membrane of GaAs with a GaAsN / GaAsN:H dot inside
  Holes are fabricated with RIE
  AlGaAs sacrificial layer removed through chemical etching
AlGaAs
GaAs
GaAsN QW
GaAs

## Slide 6: Coupling to the PhC Cavity Mode
For various cavity designs
  Close matching at low temperature was achieved between QDs and the principal cavity mode (CM)
    ~5meV mismatch at 10K
  Relative increase in the signal was observed when the QD mode approached the CM
    Between 50-70 K, one can see an increase in intensity despite the general trend of the intensity getting lower due to higher temperature

## Slide 7: Time-Correlated PL Measurements
For various cavity designs
  The spontaneous emission could be tuned based on the proximity of the QD’s mode to the CM
    Inhibited when modes are far (black dots)
    Enhanced when modes are adjacent (blue dots)
  Photon Antibunching observed
   single-photon emitter !!
mask size
d=160 nm

## Slide 8: Explanation of TCSPC Techniques
Time-resoloved PL
Second-order auto-correlation