## Slide 1
III-Sb CPV solar cells
© J.Tournet – May 2016
E. Tournie, Y. Rouillard

## Slide 2
Outline
III-Sb cells
AlInAsSb
Conclusion & outlook
1
Soitec
CPV systems

## Slide 3
III-Sb solar cells
2

## Slide 4: Interest for III-Sb compounds:
Adapted from: France et al, MRS bulletin March 2016
4J cells
3J cells
2J cells
3

## Slide 5
AlInAsSb growth
& characterization
4

## Slide 6
Sadao Adachi, 2009, Properties of semiconductor alloys, John Wiley & Sons, Ltd
Energies of the lowest direct E0 and indirect gaps EgID versus x for
AlxIn1-xAsySb1-y/GaSb and AlxGa1-xAsySb1-y/GaSb.
1.65eV
1.25eV
0.77
0.35
AlInAsSb for MJ cells
Cell type | Compo | Eg (V)
Tandem on GaSb | Al0.65In0.35As0.35Sb0.65 | 1.45
Tandem on Si | Al0.75In0.25As0.19Sb0.81 | 1.69
3J on GaSb Middle cell Top cell | Al0.53In0.47As0.45Sb0.55 Al0.75In0.25As0.27Sb0.73 | 1.21 1.68
Design by Y.Rouillard

## Slide 7
Growth strategy
6
Challenges:
Important miscibility gap for
Phase separation
Variations in composition with
Exact composition knowledge
10/2015
V2398
V2400
11/2015
Vanne As
12/2015 – 01/2016
V2428-V2448
01-02/2016
V2450-V2466
Essai bulk + DA
Lattice matching
Essais
Compo - PL
Al0,53In0,47As0,43Sb0,57
Al0,75In0,25As0,26Sb0,74
Al0,70In0,30As0,30Sb0,70
Al0,60In0,40As0,39Sb0,61
Al0,25In0,75As0,68Sb0,32
G R O W T H S R E C A P
GaSb cap @ 400°
AlSb PL @ 400°
AlInAsSb @ 400° Sb opening #2
AlInAsSb @ 400° Sb opening #1
AlSb PL @ 400°
GaSb substrate + buffer
50nm
∞
50nm
50nm
20nm
20nm

## Slide 8
Results
Experimental details:
Random alloys grown at
Test both bulk and DA
Rate 1ML/s
Capped with GaSb (impact on PL)
7
Characterization:
Lattice-matching evidenced by HRXRD
RMS roughness:
  400°C: 0,2-0,3 nm
  430°C: 0,4-0,6 nm

## Slide 9
Effect of annealing
XRD unchanged
  No phase decomposition
  No compositional variation
PL shifted towards higher energy
AlInAsSb annealed
AlInAsSb not annealed
1h
70K PL
8

## Slide 10
Conclusion
& perspectives
9

## Slide 11
Summary
Success in reproducible AlInAsSb epitaxy for various compositions
Confrontation of AlInAsSb band gap energy observations to simulation
Observation of the effect of annealing on the material
10

## Slide 12
Outlook
Improve material quality of AlInAsSb
  TEM study of AlInAsSb samples grown at different temperatures
Investigation of tunnel junctions and processing steps
Use of annealing effect to grow 2J and 3J cells
11

## Slide 13
Thank you for your attention!
Questions are welcome…