## Slide 1: PROMIS project: “Electron transport in novel Mid-IR materials and devices”
Resonant Zener tunnelling via zero-dimensional states in a narrow gap InAsN diode
Davide Maria Di Paola School of Physics and Astronomy The University of Nottingham

## Slide 2
From “conventional” to 0D - Zener tunnelling
Zener tunnelling (1934)
Band-to-band tunnelling of carriers through a forbidden energy bandgap
Esaki diode (1958)
First demonstration of quantum tunnelling in a condensed matter system
Zener, C. A.
Theory of the Electrical Breakdown of Solid Dielectrics
Proc. R. Soc. London 145, 523-529 (1934)
Esaki, L.
New Phenomenon in Narrow Germanium p-n Junctions.
Phys. Rev. 109, 603-604 (1958).
A new phenomenon:
Resonant Zener tunnelling via 0D-states in the MIR InAsN
D. M. Di Paola et al.
Resonant Zener tunnelling via zero-dimensional states in a narrow gap InAsN diode
Submitted (2016)

## Slide 3
In(AsN) Resonant Tunnelling Diodes (RTDs)
A multi-layered p-i-n RTD structure grown by MBE with an InAsN QW layer embedded between two InAlAs barries.
Optical mesa diodes and TO5 headers for electrical and optical studies

## Slide 4
Low-T current-voltage characteristics
Additional resonance features in the differential conductance.
Ohmic region at low bias voltages;
Extended negative differential resistance (NDR);

## Slide 5
Following the NDR from low to room temperature
The NDR is not observed in InAs and is weakly affected by T
Two transport processes
Thermal diffusion
Zener tunnelling
through N-related states
(50 meV below CB)

## Slide 6
Magneto-tunnelling Spectroscopy (MTS)
An e- travelling a distance s under the effect of an electric field F and a transverse magnetic field B gains
Dk ~ B
y0D
k
Sakai, J.-W. et al Probing the wave function of quantum confined states by resonant magnetotunneling, Phys. Rev. B 48, 5664 (1993)
Vdovin E.E. et al. Imaging the Electron Wave Function in Self-Assembled Quantum Dots. Science 290, 122-124 (2000)
Bx
e
Δky
Energy
Wave vector
The tunnelling current can be expressed as an overlap integral of emitter and 0D
states in k-space:
Mapping |ψ|2
in k-space

## Slide 7
Probing the size of 0D states by MTS
Coulomb potential
Parabolic potential
Patanè, A. et al. Manipulating and Imaging the Shape of an Electronic Wave Function by Magnetotunneling Spectroscopy
Phys. Rev. Lett. 105, 236804 (2010).
From modelling of the I(Bx) curves, we find that the 0D states are strongly localized (λ0 < 2 nm).
From hydrogenic model, we extract a binding energy E > 30 meV.
Interstitial N and/or vacancies induce point defects, which may be the source for the electron localization.
Strong decrease of current I with Bx
Which is the source of the 0D states?

## Slide 8
Conclusions and future studies
Modelling the effects of defects on the band structure of InAsN
Optical probing of the N-states by Electroluminescence (EL)
(in collaboration with ULAN)
Influence of growth conditions (low T) on the material quality
O’Reilly, E.P., Lindsay, A., Klar, P.J., Polimeni, A., and Capizzi, M. Trends in the electronic structure of dilute nitride alloys. Semicond. Sci. Technol. 24, 033001 (2009).
Evidence of localized states in InAsN leading to NDR
Some open questions to address require further study
MBE facilities at ULAN
Direct observation of defects (STEM)
(in collaboration with UMR)

## Slide 9: Additional information

## Slide 10
In(AsN) Resonant Tunnelling Diodes (RTDs)
Effect of doping
on the band bending
Modelling
Bound states in the QW
Activation energy Ea

## Slide 11
N-related states assisted Zener Tunnelling
Resonance:
Zener tunnelling from CB to VB
Out of resonance:
NDR

## Slide 12
Magneto-tunnelling Spectroscopy (MTS)
B//J
Weaker effect on peak D: magnetic confinement length (lz > 6.8 nm) larger than the electron confinement length (λ0 < 2 nm).
Sharpening of feature E1 and small diamagnetic shift;
Quantization in the control sample.