## Slide 1: PROMIS 2nd workshop “Modelling and design Photonics” Cadiz 18-20 May 2016
PhD student: Flavio Nucciarelli

## Slide 2
Characterization of APD devices suplied by
Sheffield University
Plasmonic for APD sensor
Sheffiled APD
Colloidal Ga NPs
NPs effect on APD
Plasmonic lens
B
A
C
Fig: ID trend related to sensors area and perimeter
We characterize the dark current of InGaAs/InAlAs APD devices supplied by Sheffiled university
It was observed how sidewalls leakage may be the most significant contribution to the dark current level in the devices

## Slide 3
Gallium nanoparticles colloidal
synthesis and investigation
Silicon substrate
Glass substrate
Sub
AZO layer
Sputtering
deposition
Sub
AZO layer
Galium
Evaporation
AZO
attack (40’’)
+
Water wash (10’)
Sub
Ultrasonication of
1.5 mL of solvent
Ga NPs
colloidal solution
or
Drop casting
(1day)
Plasmonic for APD sensor
Sheffiled APD
Colloidal Ga NPs
NPs effect on APD
Plasmonic lens

## Slide 4
Gallium nanoparticles colloidal
synthesis and investigation
We characterize the Ga NPs Abs spectrum by UV spectrophotometer
A significant absorption change was observe related to the pH value of the aqueous colloidal solution: for high acid or basic pH value of the solution, nanoparticles are less agglomerated
Water case
Plasmonic for APD sensor
Sheffiled APD
Colloidal Ga NPs
NPs effect on APD
Plasmonic lens

## Slide 5
Fabrication of patterns for selective NPs
evaporation on APD stuctures
Figure : (1) NPs on top active area (2) NPs on sidewalls area
Contact
Ga Nanoparticles
Passivation layer
Plasmonic for APD sensor
Sheffiled APD
Colloidal Ga NPs
NPs effect on APD
Plasmonic lens

## Slide 6
Plasmonic lens for APD sensor
Hole-array permit the extraordinary optical transmission (EOT) thanks to surface plasmonic polariton resonance (SPPR) and localized surface plasmonic resonance (LSPR) effects. It is possible to take advantage of EOT phenomena to fabricate plasmonic lenses.
Hole-array study by Thompson et al
We are going to investigate the hole-arrays design parameter on different materials like Au, Ga, aluminum zinc oxide (AZO) or zinc nitride.
Plasmonic for APD sensor
Sheffiled APD
Colloidal Ga NPs
NPs effect on APD
Plasmonic lens