## Slide 1: STEM investigation of dilute N containing InAs
Shalini Gupta1, Andreas Beyer1, Manoj Kesaria2, Anthony Krier2 and Kerstin Volz1
1Philipps-Universität Marburg, Faculty of Physics and Materials Science Center, Marburg, Germany
2Physics Department, Lancaster University, UK

## Slide 2: Motivation
Reference sample A0 846
[1]
Main sample A0 848 [2]
simulation
A0 846
simulation
A0 848
0.1 µm p+ InAs X1018
0.3µm p+ InAs X1017
20 nm InAs
10nm InAlAs
10nm InNAs
10nm InAlAs
20 nm InAs
0.1µm n+ InAs X1017
0.3µm n+ InAs X1018
InAs: n-type
0.1 µm p+ InAs X1018
0.3µm p+ InAs X1017
20 nm InAs
10nm InAlAs
10nm InAs
10nm InAlAs
20 nm InAs
0.1µm n+ InAs X1017
0.3µm n+ InAs X1018
InAs: n-type
[1] & [2] : Prof. Anthony Krier, Lancaster University

## Slide 3: Motivation
Reference sample A0 846
[1]
Main sample A0 848 [2]
simulation
A0 846
simulation
A0 848
0.1 µm p+ InAs X1018
0.3µm p+ InAs X1017
20 nm InAs
10nm InAlAs
10nm InNAs
10nm InAlAs
20 nm InAs
0.1µm n+ InAs X1017
0.3µm n+ InAs X1018
InAs: n-type
0.1 µm p+ InAs X1018
0.3µm p+ InAs X1017
20 nm InAs
10nm InAlAs
10nm InAs
10nm InAlAs
20 nm InAs
0.1µm n+ InAs X1017
0.3µm n+ InAs X1018
InAs: n-type
STEM measurements to investigate
Structural perfection of QWs
Abruptness of interfaces
[1] & [2] : Prof. Anthony Krier, Lancaster University

## Slide 4: Scanning transmission electron microscopy
[3] Knut Müller-Caspary, Universität Bremen
[3]
STEM uses a focused electron beam that is scanned over the sample’s surface
Incident electrons get scattered from the sample’s atoms (Rutherford scattering)
HAADF detector collects the signal from the scattered electrons
Focussed electron beam
sample
lens
HAADF detector
High angle annular dark field imaging (HAADF)  Z-contrast
recording of HAADF intensity

## Slide 5: Scanning transmission electron microscopy
STEM uses a focused electron beam that is scanned over the sample’s surface
Incident electrons get scattered from the sample’s atoms (Rutherford scattering)
HAADF detector collects the signal from the scattered electrons
JEOL JEM 2200 FS
Double- CS-corrected
recording of HAADF intensity
High angle annular dark field imaging (HAADF)  Z-contrast
[3] Knut Müller-Caspary, Universität Bremen
[3]

## Slide 6
HAADF STEM image of reference sample
InAs
InAs
InAlAs
InAs
InAlAs
Growth direction
100 nm
0.1 µm p+ InAs X1018
0.3µm p+ InAs X1017
20 nm InAs
10nm InAlAs
10nm InAs
10nm InAlAs
20 nm InAs
0.1µm n+ InAs X1017
0.3µm n+ InAs X1018
InAs: n-type

## Slide 7
InAs
InAs
InAlAs
InAs
InAlAs
100 nm
HAADF STEM image of reference sample
20 nm
Growth direction
InAs
InAlAs
InAs
InAlAs
InAs
Growth direction

## Slide 8
20 nm
Growth direction
InAs
InAlAs
InAs
InAlAs
InAs
HAADF STEM image of reference sample
5 nm

## Slide 9
HAADF STEM image of reference sample
20 nm
Growth direction
InAs
InAlAs
InAs
InAlAs
InAs
5 nm

## Slide 10
HAADF STEM image of reference sample
20 nm
Growth direction
InAs
InAlAs
InAs
InAlAs
InAs
5 nm

## Slide 11
20 nm
5 nm
5 nm
5 nm
5 nm
Quantitative Evaluation of images
Growth direction
InAs
InAlAs
InAs
InAlAs
InAs
intensity decreases

## Slide 12
5 nm
5 nm
Detection of the individual layer
5 nm
5 nm
5 nm
Determination of the individual layer-thickness at each position
Determination of the individual layer mean thickness
Relative roughness = standard deviation of thickness/mean thickness
QW
Results
Mean width = 12.4 nm
Standard deviation = 0.4 nm
Roughness = 3.6%
Mean width = 12.9 nm
Standard deviation = 0.5 nm
Roughness = 3.8 %
Mean width = 13.6 nm
Standard deviation = 0.5 nm
Roughness = 3.4 %
Quantitative Evaluation of images
20 nm
Growth direction
InAs
InAlAs
InAs
InAlAs
InAs

## Slide 13
200 nm
0.1 µm p+ InAs X1018
0.3µm p+ InAs X1017
20 nm InAs
10nm InAlAs
10nm InNAs
10nm InAlAs
20 nm InAs
0.1µm n+ InAs X1017
0.3µm n+ InAs X1018
InAs: n-type
Growth direction
InAlAs
InAs
InAs
HAADF STEM image of N containing sample

## Slide 14
HAADF STEM image of N containing sample
200 nm
0.1 µm p+ InAs X1018
0.3µm p+ InAs X1017
20 nm InAs
10nm InAlAs
10nm InNAs
10nm InAlAs
20 nm InAs
0.1µm n+ InAs X1017
0.3µm n+ InAs X1018
InAs: n-type
Growth direction
InAlAs
InAs
InAs

## Slide 15
200 nm
Growth direction
Growth direction
InAs
InAlAs
InAs
InNAs ?
20 nm
HAADF STEM image of N containing sample

## Slide 16
HAADF STEM image of main sample
200 nm
Growth direction
Growth direction
InAs
InAlAs
InAs
20 nm

## Slide 17
200 nm
Growth direction
Growth direction
InAlAs
InAs
InNAs ?
InAs
20 nm
HAADF STEM image of N containing sample

## Slide 18
200 nm
HAADF STEM image of main sample
Growth direction
Growth direction
InAlAs
InAs
InAs
20 nm

## Slide 19
20 nm
Growth direction
5 nm
HAADF STEM image of N containing sample

## Slide 20
STEM is a useful techniques to observe materials at atomic level and STEM images can be directly interpreted based on intensity.
Reference sample (no N in the QW) looks quite good i.e. seems to be grown as expected.
Many structural changes have been observed in the N containing sample.
Electron Microscopy is a useful technique to observe materials at atomic level and STEM images can be directly interpreted based on intensity.
observe materials at atomic level and STEM images can be directly interpreted based on intensity.
Summary

## Slide 21
STEM is a useful techniques to observe materials at atomic level and STEM images can be directly interpreted based on intensity.
Reference sample (no N in the QW) looks quite good i.e. seems to be grown as expected.
Many structural changes have been observed in the N containing sample.
Electron Microscopy is a useful technique to observe materials at atomic level and STEM images can be directly interpreted based on intensity.
observe materials at atomic level and STEM images can be directly interpreted based on intensity.
Summary
Future
.
Energy Dispersive X-ray Spectroscopy on N containing sample.
STEM investigation of InNAsSb/InAs sample.
Secondment to Lancaster University.

## Slide 22
Thank you for your attention!

## Slide 23
1. cleave the wafer
2. glue two parts together
3. create a block with a
thickness of 0.9 mm and
a width of 1.8 mm using
a diamond saw and glue
it into a titan pan
4. grind down the sample to
a thickness of around 100µm and polish it from
both sides.
5. create a small hole by
using the Precision Ion
Polishing System (PIPS)
1.8 mm
0.9 mm
Wafer
0.9 mm
d = 3mm
0.9 mm
500µm
Pressure
1
2
3
4
5
Cross section sample preparation
wedge shaped sample

## Slide 24
Correction of the thickness gradient in the acquired data
5 nm
5 nm
5 nm
5 nm
5 nm
QW
thickness
increases
Quantitative Evaluation of images
intensity decreases

## Slide 25
Thickness gradient corrected image
20 nm
intensity decreases