## Slide 1: APDs with ultra-thin avalanche region for sensitive X-ray detection
PROMIS
Lucas Pinel
The University of Sheffield
PROMIS Workshop
Cádiz 18-20 May 2016

## Slide 2
PROMIS
Lucas Pinel
The University of Sheffield
PROMIS Workshop
Cádiz 18-20 May 2016
Searching for the perfect profile…

## Slide 3
PROMIS
Lucas Pinel
The University of Sheffield
PROMIS Workshop
Cádiz 18-20 May 2016
Our devices
50.0 nm n In0.53Ga0.47As
100.0 nm n Al0.85Ga0.15As0.56Sb0.44
100.0 nm i Al0.85Ga0.15As0.56Sb0.44
47.0 nm p Al0.85Ga0.15As0.56Sb0.44
25.0 nm i Al0.85Ga0.15As0.56Sb0.44
25.0 nm i In0.52Al0.48As
25.0 nm i Al0.27Ga0.2In0.53As
25.0 nm i Al0.13Ga0.34In0.53As
300.0 nm i In0.53Ga0.47As
500.0 nm p In0.53Ga0.47As
300nm p In0.53Ga0.47As
100.0 nm n In0.53Ga0.47As
300.0 nm n AlAs0.56Sb0.44
80.0 nm i AlAs0.56Sb0.44
115.0 nm p AlAs0.56Sb0.44
10.0 nm i AlAs0.56Sb0.44
10.0 nm i In0.52Al0.48As
10.0 nm i Al0.27Ga0.2In0.53As
10.0 nm i Al0.13Ga0.34In0.53As
360.0 nm i In0.53Ga0.47As
500.0 nm p In0.53Ga0.47As
300nm p In0.53Ga0.47As

## Slide 4
PROMIS
Lucas Pinel
The University of Sheffield
PROMIS Workshop
Cádiz 18-20 May 2016
Our devices

## Slide 5
PROMIS
Lucas Pinel
The University of Sheffield
PROMIS Workshop
Cádiz 18-20 May 2016
Electrical characterisation

## Slide 6
PROMIS
Lucas Pinel
The University of Sheffield
PROMIS Workshop
Cádiz 18-20 May 2016
Electrical characterisation

## Slide 7
PROMIS
Lucas Pinel
The University of Sheffield
PROMIS Workshop
Cádiz 18-20 May 2016
Electrical characterisation

## Slide 8
PROMIS
Lucas Pinel
The University of Sheffield
PROMIS Workshop
Cádiz 18-20 May 2016
Summary of progress
Etching recipe improvement:
  Better reproducibility
  Less edge breakdown
Better doping control in AlAsSb layer
Working photodiodes with low gain

## Slide 9
PROMIS
Lucas Pinel
The University of Sheffield
PROMIS Workshop
Cádiz 18-20 May 2016
Future work
Need for better control of dopant (Be) activation in AlAsSb layer => try annealing
Testing working diodes with X-ray
Planar diodes to overcome etching difficulties