## Slide 1: Dilute Nitrides for the Mid-infrared
A. Krier, M. Kesaria, Q. Zhuang
Physics Department Lancaster University, UK
A .V. Velichko, O.Marakovsky, D. Paola, A. Patane
School of Physics and Astronomy, University of Nottingham, UK
A. Polimeni, S. Birindelli, M. Capizzi
Physics Department, CNISM, Sapienza Università di Roma, Italy
PROMIS Summer School
Montpellier 2016

## Slide 2: Outline
  Motivation
  MBE growth on InAs and GaAs
  Structural and optical properties
  Annealing and Hydrogenation
  Devices
N

## Slide 3: Motivation
Gas sensors - optical absorption;
CH4, CO2, CO
Industrial process control
Spectroscopy
Thermal imaging
Bio-medical diagnostics
Free space optical communications
(3-5 μm)
Military - infrared countermeasures
Principal gas absorptions in the mid-infrared
For these applications we need LEDs, lasers and detectors operating at Room Temperature

## Slide 4: Mid-infrared - main challenges
imbalance in the DOS of InAs
Auger recombination (CHSH)
Inter-valence band absorption (IVBA)
Inadequate electrical confinement
small band offsets
No SI substrates
Addition of N :
- flexible wavelength tailoring
without complex growth
- de-tuning of CHSH resonance
Auger suppression
InAsN dilute nitride alloys offer some possibilities for improvement??
2’
1’
2
1
CB
LH
HH
Eg
Δ0

## Slide 5
W. Shan et al., Phys. Rev. Lett. 82, 1221 (1999)
An empirical model
ECB
EN
E+
E-
Extended-localized state interaction
Anticrossing/repulsion between conduction-band edge and localized states
decreases the band gap
introduces minigap(s) at low k-value in the CB
Band anti-crossing
GaAsN

## Slide 6
Dilute nitrides
Harris, J. S. Semiconductor Science and Technology 17, 880 (2002)
N introduces tensile strain (on InAs or GaAs)
disorder and strong bowing
D. Sentosa, X. Tang,a, and S.J. Chua, Eur. Phys. J. Appl. Phys. 40, 247–251 (2007)
N
InAs
InN

## Slide 7
MBE Growth on InAs and on GaAs
V80 Molecular Beam Epitaxy (VG)
with RF Plasma Nitrogen source, As and Sb valved cracker cells (EPI)
Ga, In, Al and dopants GaTe and Be
Large parameter space for InAsN
InAsN successfully grown on InAs with N < 2% and PL observed out to 4.5 µm
For growth on GaAs
Optimum growth at substrate temperatures between 4000C- 4400C
Nitrogen plasma setting fixed at 160 W with flux of 5x10-7 mbar
Growth rate of ~1µm per hour
InAs control sample was grown under the same conditions
Sample | TG | Flux - As | Flux - N2 | Plasma Power | N Content %
A0276 | 485 | 6.6x10-6 | n/a | n/a | n/a
A0282 | 420 | 2.2x10-6 | 6.12x10-7 | 160 | 0.6
A0285 | 442 | 2.2x10-6 | 6.12x10-7 | 160 | 0.2
A0299 | 376 | 2.2x10-6 | 6.3x10-7 | 160 | 1.0
A0300 | 450 | 2.8x10-6 | 5.0x10-7 | 160 | 0.4

## Slide 8
X-ray diffraction
N=0.83% - tail indicates vertical N composition gradient
N=0.34% - thickness fringes – good interface quality
Growth rate decreases with increasing N
asymmetrical (224) reflections obtained for all samples
2 different layer peaks obtained - 2 dominant N compositions
Plastic relaxation
Vertical and horizontal lattice deformations obtained
Gives relaxed lattice const.
and plastic deformation R
Layers with N< 1.2% are pseudomorphic
Bragg maps narrow in qII
N > 1.2% more diffuse scattering from misfit dislocations & defects
Onset of plastic relaxation at N~ 1.4%

## Slide 9
Chart: Sample : A0299 InAsN 1% N
SIMS and TEM analysis
N is uniform
No evidence of unintentional impurities (C, O etc.) as-grown InAsN is of high purity
Analysis of secondary ion peaks from CsAsN+ enables accurate N determination
-comparison with XRD data – N content is ~5% larger than determined from XRD
Significant incorporation of non-substitutional N
Higher dislocation density in InAsN – but obtain increase in PL
Localisation, non-uniform PL emission from regions around dislocations?
InAs/GaAs
InAsN(1%) /GaAs
200 nm
200 nm
As
In
N
Ga

## Slide 10
Raman spectroscopy
Weak InAs modes at 405 and 425 cm−1 and
2nd order InAs optical modes at 435, 450, 460 and 480cm−1
Additional N related features at 402, 415, 428 and 443 cm−1
(Wagner et al. N ~ 1.2 %)
difference spectrum of highest N – lowest N content
443 cm−1 feature - also detected in FTIR
NAs LVM from substitutional 14NAs
402 cm−1 and 415 cm−1 peaks from non-substitutional N-N or As-N split interstitials, (N antisites or interstitial N) rather than N-In-N complexes
and As -N produce deviations from Vegard’s law
(Calculations predict N-N split interstitial at 419 cm−1
but also predict that the As-N split interstitial lies well above the LVM in GaAsN)
N related features
NAS
As -N
N-N
Ibanez et al, JAP (2010)
2nd order InAs modes

## Slide 11
N reduces electron mobility
µ is limited by electron scattering by N-atoms, -pairs and clusters
Model for GaAsN predicts a strong reduction of the mobility and electron mean free path due to the N-levels
Weak dependence of µ on N-content compared to GaAsN due to the proximity of the N-related states to the CBE
Impurity scattering dominant at high N
Residual carrier conc. increases for N >0.4%
N incorporation introduces native donor states
Electrical properties InAsN on GaAs
A. Patanè et al Appl. Phys Lett. 93, 25106 (2008)
Phonon scattering
impurity scattering
1000 nm n-type InAs(N)
Semi-insulating GaAs substrate

## Slide 12
The increase of electron density with increasing N indicates a pinning of the Fermi level and implies a substantial density of native donor states
InAsN - Cyclotron Resonance
O. Drachenko et al. APL 98, 162109 (2011)
Pinning of the Fermi level

## Slide 13
Photoluminescence InAsN on InAs
Incorporation of small amounts of N into III-V’s causes conduction band anti-crossing leading to reduction in band gap
Good agreement with band anti-crossing model
(60 meV per 1%N)
Long low energy tail appears - localisation
CMN = 2.5 eV at 4 K
caused by uneven nitrogen distribution- composition fluctuations or point defects

## Slide 14
J. Appl. Phys. 108, 103504 (2010)
PL is Gaussian at low T
As T increases becomes asymmetric with high energy tail
extends well above Eg
Lineshape - 2 effects
Localization at low T
Free carrier emission at high T
Photoluminescence Lineshape
Conduction Band
Valence Band

## Slide 15: PL analysis temperature dependence
InAsN(1%) exhibits very weak temperature quenching ~ 8x
PL emission obtained up to room temperature without annealing
Peak wavelength near 4 µm – appropriate for CO2 detection

## Slide 16: InAsN Photoreflectance
Where, x is the N content
Solid lines are fits to
N does not change Δso

## Slide 17
PL obtained from InAsN on GaAs across the mid-IR spectral range with addition of small quantities (~ 1%) of nitrogen
Good agreement with band anti-crossing model
Inclusion of nitrogen improves the peak intensity InAsN > InAs on GaAs
Photoreflectance shows Δ0 is constant with increasing N
Activation energy increases with increasing N content – CHSH Auger detuning
InAsN on GaAs
4K PL
improved PL

## Slide 18: Adding Sb - MBE growth of InAsSbN
N is hard to incorporate
Use Sb to reduce lattice mismatch increase N incorporation improve quality
InAs
Conduction band
Valence band
Increasing N
Tensile strain
Increasing Sb
Compressive strain
Adding N to InAs
Adding Sb to InAs
Eg
Sb acts as surfactant to maintain 2D growth and reduces point defects - improves PL
Red-shift of emission wavelength
– need less N to reach longer wavelengths
Sb reduces N surface diffusion length - increases N incorporation ~ 2.5x
Reduction of Sb segregation induced by N - increases Sb incorporation ~1.5x

## Slide 19
Photoreflectance
Kudrawiec et al. APL 99, 011904 (2011)
Δso > E0 Auger suppression
Advantage of InAsNSb over InAsN
In-plane strain for layers grown on InAs
can be tuned from tensile to compressive
- Tailor polarization in QW to be either TE or TM
Sb increases confinement in valence band
- dominant polarisation is TE (e1-hh1)
Spin orbit splitting In InNAs & InAsNSb
Incorporation of Sb increases Δso and decreases E0
N does not change Δso
Both Sb and N reduce E0
~ 5 meV per 1% of Sb
~ 60 meV per 1% N

## Slide 20
Strong PL at room temperature
- good optical quality
Asymmetric shape
Narrow energy gap – free carrier emission is important
Especially > 100 K
High energy tail extends well above Eg
Gaussian at low T
PL peak lower than Eg determined from PR
Characteristic S-shape but with weak carrier localisation
Stokes shift <10 meV
smaller than for InAsN
Composition fluctuations or point defects reduced due to surfactant effect of Sb
InAsSbN Photoluminescence
Latwoska et al, Appl. Phys. Lett 102, 122109 (2013)

## Slide 21
Fit using
Includes localized and band-band transitions
A = scaling factor
Ecr = energy of crossover between equations
K = smoothing parameter
σ relates to slope of DOS
Set K = kBT/σ and Ecr = Eg + kBT/σ
n= 0.5 to 2 for momentum conserving non-conserving transitions
Best fit when n=1
Black arrows – Eg determined from PL fitting
Red arrows – PL peak
Note the difference which increases with T
Photoluminescence curve fitting
Latwoska et al, Appl. Phys. Lett 102, 122109 (2013)

## Slide 22
Comparison of change in energy gap with T
InNAsSb 65 meV
InAs 66 meV
InSb 62 meV
whereas 1% N in GaAs reduces T dependence of Eg by 40%
Temperature dependence of bandgap
BAC model gives good agreement
T dependence of Eg in InNAsSb is not
sensitive to N due to large separation between EN and EM (~ 1 eV)

## Slide 23
Rapid thermal annealing of InAsN/GaAs
Rapid thermal annealing (RTA): 30 sec in N2
4K PL enhanced by 25-30 times due to a reduction in SRH recombination
RT PL intensity increased only moderately
RTA causes reduction in point defects but not in Auger recombination
Slight blue shift (10 meV) in PL emission peak energy: due to small decrease in N ~0.1%

## Slide 24
4K PL enhanced by 25-30 times due to reduction in SRH recombination
Slight blue shift (17 meV) in PL emission peak energy: due to decrease in N ~0.15%
Kesaria, M. et. al . Infrared Physics & Technology 2015, 68, 138-142
Increase in PL efficiency of RTA InAsN/InAs

## Slide 25
Eg(T)=Eg(0)
Varshni fit
β =100-110 K
α =510-4 (eV/K)
Eg(0)=0.343-0.349 eV
RTA reduces localisation and improves N compositional uniformity
Conduction Band
Valence Band
Introduction of N reduces thermal quenching
But, RTA increases thermal quenching rate
Localisation is reduced
Passivation of localized states & Temperature Quenching
InAsN(1%)/GaAs
InAsN(1%)/GaAs
as-grown
InAs/GaAs

## Slide 26
H irradiation - Increase in PL efficiency
TH = 250 C
H-dose H0 = 1×1016 cm-2
[N]=0, InAs
PL efficiency first increases with H dose, reaches a maximum value
then it saturates and decreases at higher H doses
The same behavior is observed for [N]≠0, In(AsN)
Notice that hydrogenation conditions and H doses resulting in maximum increment in PL efficiency depend on [N]

## Slide 27
Hydrogen diffusion and trapping: SIMS
[H]=10×1016 cm-2
X-TEM images highlight a non-homogeneous concentration of threading dislocations at the InAs/GaAs highly mismatched interface
TH = 250 C
[N]=1.1%
[H]=1×1016 cm-2
X-TEM
D diffuses see inset to the InAs/GaAs interface, where it is trapped and accumulates
D diffuses and traps (at N sites)
D does not reach the InAs/GaAs interface
[N]=0

## Slide 28
Hydrogenated samples:
- PL efficiency increases
localized states are passivated, Epeak
increases
- a sizable RT emission is achieved
[H] = 1×1016 cm-2
Temperature (K)
As-grown samples:
High density of localized states
S-shaped of Epeak vs T
- RT emission is not achieved
Passivation of localized states

## Slide 29
Thermal recovery of the as-grown PL efficiency
[N]=1.1%
[H] = 1×1016 cm-2
Two activation energies two different nonradiative defects are passivated by H
attempt frequency value typical of N-H local modes

## Slide 30
InAsN QW lasers on InP
InAsN ridge lasers operating up to 2.6 µm have been demonstrated – grown by gas source MBE
limited by N incorporation and critical thickness
4 QW InAsN/InGaAs on InP (5μs pulse width, 500 Hz repetition rate)
Max. operating temperature 260 K with T0 = 110 K
Decreasing growth temp incorporates more N
….but reduces QW quality
D. K. Shih, H, H. Lin, and Y. H. Lin, IEE Proc. Optoelectronics 150, 253 (2003)

## Slide 31: InAsSbN / InAs MQWs
200 nm InAs Buffer Layer
InAs substrate
100 nm InAs Capping Layer
10x InAsNSb /InAs QW
(12x24 nm)
Growth of the MQWs calibrated using the same growth method of previously grown InAsNSb bulk layers
200 nm InAs Buffer layer grown at 480°C
10x InAsSbN/InAs QW grown at 420°C
  Growth rate of 0.5µm per hour
  Nitrogen plasma setting fixed at 160 W with flux of 6×10-6 mbar
100 nm InAs Capping Layer grown at 480°C
As flux kept at minimum for growth of InAs layers

## Slide 32: InAsSbN/InAs MQW 4K photoluminescence
No blue-shift with excitation power - Type I QW
Band alignment determined by modification of InAsSb - Type II alignment with conduction and valence band offsets of 39 & 82 meV
ADDITION OF N :
  Reduction in overall strain Reduction of
  band gap
  Conduction band further reduced by BAC model
  Reduction of 63 meV
3.62 µm (expt.)
3.48 µm
N =1%, Sb 6%

## Slide 33: InAsSbN MQW LED
p-i-n diode containing 10x
InAsSbN QW in active region N =1%, Sb 6%
Longest wavelength dilute nitride
light emitting device to date
InAs (100) substrate
n InAs
p InAs
C-H
absorption
300 K EL
n+-InAs
p+-InAs
InAsNSb MQW
4 K EL
LED output power : 6 µW at 100 mA drive current and internal RT efficiency ~ 1%
InAsSbN e-hh1
InAsSb e-hh1
InAsSb e-hh2

## Slide 34: Comparison with InAsSb
InAsSbN MQW LED
N =1%, Sb 6%
Comparison of the temperature dependence of the EL with that of type II InAsSb/InAs reveals more intense emission at low temperature
Improved temperature quenching up to T~200 K where thermally activated carrier leakage becomes important and further increase in the QW band offsets is needed
Increasing the nitrogen content above 0.5% reduces the band gap sufficiently such that the energy gap Eo becomes less than Δso effectively detuning the CHSH Auger recombination mechanism
InAsSbN e-hh1
InAsSb e-hh1
InAsSb e-hh2

## Slide 35
R0A ~1/n
InAsSbN MQW p-i-n photodetector
Cut-off λ ~ 4 μm
Ideality factor = 1.6
R0A
T<120 K generation-recombination dominates
T>220K diffusion limited recombination is dominant
Capacitance at 0V =2.54 nF
Built in potential = 0.19 V
Carrier concentration = 8.3x1017 cm-3
R0A ~1/n2

## Slide 36
In(AsN) Resonant Tunnelling Diodes (RTDs)
A multi-layered p-i-n RTD structure grown by MBE with an InAsN QW layer embedded between two InAlAs barriers.
Optical mesa diodes and TO5 headers for electrical and optical studies

## Slide 37
Low-T current-voltage characteristics
Additional resonance features in the differential conductance.
Ohmic region at low bias voltages;
Extended negative differential resistance (NDR);

## Slide 38
Following the NDR from low to room temperature
The NDR is not observed in InAs and is weakly affected by T
Two transport processes
Thermal diffusion
Zener tunnelling
through N-related states
(50 meV below CB)

## Slide 39
Magneto-tunnelling Spectroscopy (MTS)
An e- travelling a distance s under the effect of an electric field F and a transverse magnetic field B gains
Dk ~ B
y0D
k
Sakai, J.-W. et al Probing the wave function of quantum confined states by resonant magnetotunneling, Phys. Rev. B 48, 5664 (1993)
Vdovin E.E. et al. Imaging the Electron Wave Function in Self-Assembled Quantum Dots. Science 290, 122-124 (2000)
Bx
e
Δky
Energy
Wave vector
The tunnelling current can be expressed as an overlap integral of emitter and 0D
states in k-space:
Mapping |ψ|2
in k-space

## Slide 40
Summary
Successful MBE growth of InAsN directly onto InAs and GaAs substrates with N up to ~ 2%
Behaviour of N in InAs different to N in GaAs
Fermi level pinning and native donor states
PL covers the mid-infrared (2-5 μm) spectral range in good agreement with the BAC model
Localisation and free carrier effects are important in interpretation of PL spectra
N reduces band gap but has little effect on T sensitivity
Photoreflectance shows N has no effect on Δo , Auger CHSH de-tuning is possible
Addition of Sb increases N incorporation –structural and optical properties
- improved and bright PL obtained from Type I InAsSbN/InAs MQWs
First long wavelength dilute N LED operating at 300 K
good prospects for device applications if electron concentration can be controlled

## Slide 41
RTA reduces native point defect concentration & improves material uniformity
4K PL intensity increased by ~ 20x
Elimination of deep fluctuations in conduction band leads to reduced localization in annealed samples but causes an increase in thermal quenching
Increasing doses of H irradiation of In(AsN) leads to a passivation of localised states
and an increase in PL efficiency ~20x at low H doses
First InAsN resonant tunnelling diodes – MTS to probe localised defect states

## Slide 42
Acknowledgements
  A. Patane Nottingham University Transport measurements
  R. Beanland & A. Sanchez University of Warwick TEM
  J. Ibanez University of Madrid Raman spectroscopy
  R. Kudrawiec Institute of Physics, Wroclaw Photoreflectance
O. Drachenko Helmholtz-Zentrum
M. Helm Dresden-Rossendorf Cyclotron resonance studies
M. Schmidbauer Leibniz-Institute, Berlin X-ray diffraction measurements
  S. Birindelli, M. De Luca,
  A. Polimeni and M. Capizzi CNISM and Physics Department Hydrogenation studies
  Sapienza Università di Roma, Italy
  We are grateful for financial support provided from EPSRC (EP/J015849/1) and the EU Marie Skłodowska-Curie ITN -PROMIS (H2020-MSCA-ITN-2014-641899)