## Slide 1
Antimonide materials and devices
Eric Tournié
University of Montpellier and CNRS, France
Institut d’Electronique et des Systèmes, UMR 5214
eric.tournie@umontpellier.fr

## Slide 2: Outline
Antimonide-based compound semiconductors (ABCS)
InAsSb/InAs and InSb/InAs mid-IR LEDs
GaSb-based laser diodes: edge-emitting diodes and VCSELs
InAs/AlSb quantum-cascade lasers
GaSb/InAs type-II superlattice photodetectors
ABCS compounds for plasmonics and solar cells ?
Conclusion – perspectives

## Slide 3: Outline
Antimonide-based compound semiconductors (ABCS)
InAsSb/InAs and InAs/InSb mid-IR LEDs
GaSb-based laser diodes: edge-emitting diodes and VCSELs
InAs/AlSb quantum-cascade lasers
GaSb/InAs type-II superlattice photodetectors
ABCS compounds for plasmonics and solar cells ?
Conclusion – perspectives

## Slide 4
The semiconductors based on GaSb, InAs, AlSb, InSb and their alloys:
AlGaAsSb, GaInAsSb, AlGaInAsSb…
Generally grown on GaSb or InAs substrates
Antimonide-based compound semiconductors (ABCS)
These compounds are also known as the "6.1Å SC" , the "GaSb technology"

## Slide 5
Large bandgap range :
        0.1 – 2 eV
 Band gap engineering
Large band offsets:
Ec = 0 – 2 eV
Ev = 0 – 0.5 eV
Various band alignments:
Type I, Type II, Type III
Antimonide-based compound semiconductors
Large lattice parameter range:
 Lattice matching is an issue
AlSb
GaSb
0.18 eV
0.72 eV
InAs
1.6 eV
X
a ~ 6.1 Å
6.47 Å
0.36 eV
InSb
GaAs
1.4 eV
2.2 eV
AlAs
5.65 Å
 Band offset engineering

## Slide 6
 | AlAs | AlSb | GaAs | InP | GaSb | InAs | InSb | Si | Ge
me* / m0 | 0.083 | 0.102 | 0.066 | 0.073 | 0.042 | 0.023 | 0.014 | 0.15 | 0.044
mhh* / m0 | 0.409 | 0.336 | 0.377 | 0.6 | 0.222 | 0.26 | 0.244 | 0.54 | 0.28
µe (300 K) (cm2. V-1.s-1) |  |  | 8500 | 5400 | 3000 | 40 000 | 77 000 | 1400 | 3900
µh (300 K) (cm2. V-1.s-1) |  |  | 400 | 200 | 1000 | 500 | 850 | 450 | 1900
Low masses, high mobilities….
ABCS: effective masses, mobilities

## Slide 7
ABCS: no common atom interfaces
InAs/AlSb
Some materials combinations exhibit no-common atom interfaces:
  GaSb / InAs
  AlSb / InAs
 Careful Interface engineering
GaSb (9 MLs)
InAs (9 MLs)
InSb
d {111}

[100]
TEM: A. Trampert, PDI-Berlin
InAs/GaSb

## Slide 8
No common atom InAs / GaSb superlattice: interfaces matter!!
InAs 4 ML
GaSb 3 ML
InSb 1 ML
GaSb 3 ML
In |  | On |  |  | On |  | 
As |  |  |  |  | On |  | 
Ga | On |  | On |  |  |  | On
Sb | On | On | On |  |  | On | On

## Slide 9
GaInAsSb alloy
Large miscibility gaps: metastable and unstable alloys…
Antimonide-based compound semiconductors

## Slide 10
ABCS compounds and heterostructures:
    “low temperature” materials: Tm(InSb) = 515 °C, Tm(GaSb) = 712 °C (GaAs: 1238 °C)
      low temperature growth: 400 °C < Tg < 520 °C
  Unstable/metastable compounds
  High-Al content in many devices
  Lack of MOVPE developments (efforts starting in the US?)
Molecular-beam epitaxy (MBE) is the only growth technique giving high-quality heterostructures (till now).
GaSb and InAs substrates:
  always conductive
  2 to 4 inch, 5 inch under development
  few producers of good quality substrates: high price (~400 €/ 2 inch)
  thermal deoxydation remains an issue
Doping properties:
  Si = p-type dopant in III-Sb compounds but InAs and InSb
  Te = preferred n-type dopant
  Be = p-type dopant
Antimonide-based compound semiconductors

## Slide 11
ABCS are well adapted to:
high frequency, low power devices
opto devices operating the IR, particularly mid- and far- IR
Antimonide-based compound semiconductors
Unrivaled band gap range 
Large band offsets 
Type I to type III alignments 
Low effective masses 
Two group-V elements   
No common atom interfaces   
Complex (quat-/pent-anary) alloys 
Large mismatch range (-8% / +7 %) 

## Slide 12
Mid-IR
Transparence windows of the atmosphere
Strong absorption lines of many “interesting” gases
The mid infra-red

## Slide 13: Outline
Antimonide-based compound semiconductors (ABCS)
InAsSb/InAs and InSb/InAs mid-IR LEDs
GaSb-based laser diodes: edge-emitting diodes and VCSELs
InAs/AlSb quantum-cascade lasers
GaSb/InAs type-II superlattice photodetectors
ABCS compounds for plasmonics and solar cells ?
Conclusion – perspectives

## Slide 14
Type-II InAsSb/InAs mid-IR LEDs
Carrington et al. SST 24, 075001 (2009)
See WP4 discussion

## Slide 15
Type-II InSb/InAs mid-IR LEDs
Zhuang et al. J. Phys D 41, 232003 (2008)
See WP4 discussion

## Slide 16: Outline
Antimonide-based compound semiconductors (ABCS)
InAsSb/InAs and InSb/InAs mid-IR LEDs
GaSb-based laser diodes: edge-emitting diodes and VCSELs
InAs/AlSb quantum-cascade lasers
GaSb/InAs type-II superlattice photodetectors
ABCS compounds for plasmonics and solar cells ?
Conclusion – perspectives

## Slide 17
The basic device in the GaSb technology: typical band-structure design
Lattice-matched Al0.9Ga0.1As0.08Sb0.92 cladding layers
Lattice-matched AlGaAsSb or AlGaInAsSb waveguide
Strained ( ~1.5 – 2%) GaIn(As)Sb quantum wells
GaSb-based type-I QWs laser diodes
Growth direction
Energy
Ga1-xInxAsySb1-y QWs
AlGaAsSb or AlGaInAsSb
waveguide
~0.8 µm
Al0.9Ga0.1As0.07Sb0.93:Te
Lower cladding
Al0.9Ga0.1As0.07Sb0.93:Be
Upper cladding
GaSb :Te Substrate
GaSb:Be p-type contact layer
~1.5 µm
~1.5 µm

## Slide 18
2 µm < λ < 3 µm: GaInAsSb / AlGaAsSb (quaternary materials)
3 µm < λ: GaInAsSb / AlGaInAsSb (quaternary/pentanary materials)
GaSb-based type-I QWs laser diodes: band-offset management

## Slide 19
GaSb-based type-I QWs laser diodes
Fabry-Perot laser diodes cover the whole 1.5 – 3.3 µm wavelength range
Pout  when 
See, e.g., Tournié & Baranov, Semiconductors and Semimetals, vol. 86, pp. 183 – 226 (2012).
Gad et al., Semicond. Sci. Technol. 28 (2013) 015015

## Slide 20
Gaimard et al. , Appl. Phys. Lett. 104, 161111 (2014)
2nd order DFB
Buried Grating GaSb-based DFB lasers

## Slide 21
10 x 900 µm
1st order DFB, L = 485 nm, duty 50 %
15°C:
Threshold current: 220 mA
Optical power per facet: 2 mW
Same values on FP lasers from the same wafer
SMSR = 30 dB
Total continuous tuning for a fixed T : 2.5 nm
I
T
Buried Grating:  ~ 3 µm
Gaimard et al., Opt. Express 23, 19118 (2015).

## Slide 22
6 µm apertured monolithic GaSb VCSEL @ 2.3 µm
CW operation up to 70°C
Threshold ~ 1.9mA at 30°C
Single mode with SMSR > 20dB
Large tunability ~14 nm
Max output power 100 µW at 10°C
Sanchez et al., Opt. Express 20, 15540 (2012).
6 µm

## Slide 23: Outline
Antimonide-based compound semiconductors (ABCS)
InAsSb/InAs and InSb/InAs mid-IR LEDs
GaSb-based laser diodes: edge-emitting diodes and VCSELs
InAs/AlSb quantum-cascade lasers
GaSb/InAs type-II superlattice photodetectors
ABCS compounds for plasmonics and solar cells ?
Conclusion – perspectives

## Slide 24
Key parameters : ΔEc =2.3 eV
m*=0.023
ΔL=0.8 eV
High gain
Short wavelength
Long wavelength
m*=0.023
m*=0.045
m*=0.067
InAs/AlSb: very good intrinsic properties for QCLs
Gain in QCL

## Slide 25
Short wavelength InAs/AlSb QCLs
3 µm
More details on InAs/AlSb QCLs in: Teissier, Baranov, et al.

## Slide 26
PROMIS – Workshop - Sheffield
Total thickness 21 µm. Growth time ~ 24h…
50 μm
Long wavelength InAs/AlSb QCLs (dielectric waveguide)
Bahriz et al., Opt. Expr. 23, 1523 (2015)
Jth = 4.3 kA/cm² at 300 K / P (80 K) ≈ 120 mW / P(300 K) ≈10 mW / Tmax = 353 K
Notes: Compromis entre faible perte et recouvrement avec la zone active
Simplification du process
Spacer peu dopé

## Slide 27
0.3 ML AlSb barrier
12 nm
3-2
2-1
3-2
2-1
=> Very thin barrier acts
in good agreement with calculation
TEM image from D. Alloyau, C. Ricolleau, G. Wang (MPQ, Univ Paris Diderot)
InAs/AlSb QCLs: growth control

## Slide 28: Outline
Antimonide-based compound semiconductors (ABCS)
InAsSb/InAs and InSb/InAs mid-IR LEDs
GaSb-based laser diodes: edge-emitting diodes and VCSELs
InAs/AlSb quantum-cascade lasers
GaSb/InAs type-II superlattice photodetectors
ABCS compounds for plasmonics and solar cells ?
Conclusion – perspectives

## Slide 29
Buffer GaSb (p)
InAs (n)
GaSb (p)
Iph
A
h
InAs/GaSb
SL
SL : active zone of a pin junction
 PV detector
Cut-off tuning from SWIR to VLWIR
depending of SL’s period (InAs+GaSb layers)
VLWIR
MWIR
LWIR
GaSb (40Å) (3Å=1ML)
GaSb/InAs superlattice photodetector

## Slide 30
GaSb/InAs superlattice photodetector
Manurkar et al. Appl. Phys. Lett. 97, 193505 (2010): Razeghi’s group, Northwestern Uni, USA
1kx1k FPA, lC = 11 µm
substrat GaSb (N) 3’’
Jdark= 3.3x10−4 A.cm−2, QE = 78%
State of the art pixels
Cf. Christol, Rodriguez, et al.

## Slide 31
31
31
GaSb/InAs superlattice photodetector

## Slide 32
Same cut-off wavelength but very different spectral responses and electrical properties…
GaSb-rich
R = 0.5
InAs-rich
R = 2
Symmetric
R=1
GaSb/InAs superlattice photodetector
Origin ?
Impact on detector performances ?
 Under study !
Christol et al., SPIE Proc. 9370, 93701Z (2015)

## Slide 33: Outline
Antimonide-based compound semiconductors (ABCS)
InAsSb/InAs and InSb/InAs mid-IR LEDs
GaSb-based laser diodes: edge-emitting diodes and VCSELs
InAs/AlSb quantum-cascade lasers
GaSb/InAs type-II superlattice photodetectors
ABCS compounds for plasmonics and solar cells ?
Conclusion – perspectives

## Slide 34
InAsSb:
Lattice-matched onto GaSb
High-doping level (> 5 x1019 cm-3)
Low effective mass
‘‘All-semiconductor’’ plasmonics
500 nm
535 nm
[001]
[110]
[110]
(a)
GaSb
GaSb
InAsSb
See WP4 discussion
Taliercio et al., Opt. Express, to be published.

## Slide 35
GaSb-based solar cells
Mechanically stacked GaAs/GaSb tandem cells
= 31% @ 100 suns
Bett et al., Appl. Phys . A 69, 119 (1999)
Intermediate band solar cells (U Lancaster)
See WP3 discussion
III-Sbs cover the whole bandgap range adapted to multi-junction solar cells.

## Slide 36: Outline
Antimonide-based compound semiconductors (ABCS)
InAsSb/InAs mid-IR LEDs
GaSb-based laser diodes: edge-emitting diodes and VCSELs
InAs/AlSb quantum-cascade lasers
GaSb/InAs type-II superlattice photodetectors
ABCS compounds for plasmonics and solar cells?
Conclusion – perspectives

## Slide 37
The GaSb technology has been progressively maturing in the last decade.
Various designs are available to cover the whole MIR wavelength range:
  Type-I QW laser diodes or VCSELs: 2 – 3.5 µm
  Type II QWs or QDs LEDs: > 3.5 µm
  QCLs: 3 – 20+ µm
  ICLs: 3.5 – 6 µm (see Vurgaftman et al., J. Phys. D. 48, 123001 (2015)).
High performance MWIR photodetectors
Conclusion
July 2015
QW/QD GaAs
QW/QD InP
QW GaSb: CW
QCL InP
QCL GaAs
IBCL GaSb: CW
QCL InAs/AlSb: pulsed
1
 (µm)
2
3
5
4
20
on Si
QW GaN
9

## Slide 38
Perspectives
Mature buried-grating DFB lasers
Extend  beyond 20 µm with InAs/AlSb QCLs
LWIR photodetectors
Integrate GaSb-based devices on Si and SOI
Extend bandgap range with dilute nitride or bismide alloys
……………………………………………………………
Demonstrate PROMISed devices
Thank you for your attention

## Slide 40
Antimonide-based optoelectronic devices
GaInAsSb / AlGa(In)AsSb type-I QWs
  Edge-emitting laser diodes: 1.5 – 3.4 µm
  VCSELs: 2 – 2.6 µm
GaInSb /InAs « W » QWs
  Interband cascade laser diodes: 3.5 – 6 µm
AlSb /InAs type-II QWs
  Quantum cascade lasers: 2.6 – 20 µm
GaSb /InAs type-III superlattices
  photodetectors: 2 – 30 µm

## Slide 41
Introduction of a Bragg grating to modulate the refractive index along the waveguide :
Amplification of the optical mode with the same periodicity
Coupled modes theory :
  Coupling efficiency :  (cm-1)  strongly related to the grating geometry
Distributed-feedback (DFB) lasers for single-frequency emission

## Slide 42
Losses-coupling (Da)
Index-coupling (Dn)
Δneff
Buried grating usual with InP lasers
GaSb lasers: no attempt yet
Semiconductor devices: 2 types of coupling
Lateral direction
Longitudinal direction
Transverse direction
Complex (Cr) LC-DFB
grating
DFB lasers: coupling effects
©

## Slide 43
SMSR = 25 dB
Tuning range = 3 nm
CW operation up to 38°C
Ith = 80 mA @ 20°C
Pmax = 3 mW
SMSR > 35 dB
Tuning range = 2.5 nm
CW operation up to 38°C
Ith = 90/140 mA @ 10°C/20°C
Pmax = 1.7 mW à 10°C
Naehle et al., Electron. Lett., 47, 46 (2011)
GaSb-based DFB lasers: loss coupling
LPN
Works well but:
low output power
complex processing
Barat et al., App. Phys. B 90, 201 (2008)

## Slide 44
Grating order: need of a compromise!
  High order  more diffraction losses BUT easier technology implementation
   depends on order and duty cycle
Parameters chosen to get L ~ 1.25, with :
2nd order ( = 2  2.7 µm)
1st order ( = 3 µm)
GaSb-based DFB lasers: buried grating
Lower Cladding
Waveguide
Mesa

## Slide 45
40dB
10 X 650 µm
2nd order DFB, L = 696 nm, duty 70%
15°C:
Threshold current: 35mA
Optical power per facet: 25 mW
Same values on FP lasers from the same wafer
SMSR = 40 dB
Total continuous tuning for a fixed T : 4.5 nm
Buried Grating:  ~2.4 µm
Gaimard et al., Opt. Express, to be published

## Slide 46
MBE growth of the monolithic VCSEL:
  total thickness ~ 12 – 15 µm (14 – 17 hours growth)
Lateral selective etching of TJ (Sanchez et al., SST 27, 085011 (2012))
Apertured VCSEL Process
Top epitaxial n-DBR
AlAs0.08Sb0.92/GaSb 20 pairs: (R > 99.8%)
top-contact
Active region:
- 5 x Ga0.65In0.35As0.1Sb0.9 QW - Al0.35Ga0.65As0.03Sb0.97 barriers
(1-2% lattice mismatch)
Bottom epitaxial n-DBR
24 pairs AlAs0.08Sb0.92/GaSb
n ~ 0.6  R > 99.9%
back-contact
n-GaSb substrate
Apertured TJ
n+ InAs/ p+ GaSb
Light
Apertured GaSb VCSELs
PROMIS – Workshop - Sheffield

## Slide 47
Cascaded GaSb VCSELs
CW operation up to 70°C
Max output power 1 mW
WPE ~5 %
Sanchez et al., PTL 25, 882 (2013); J. Phys D 46, 495101 (2013)

## Slide 48
Interband cascade lasers (ICLs): band diagram
(NRL, USA; U. Würzburg, Germany)
Revue: Vurgaftman et al., J. Phys. D, 48, 123001 (2015).
1st Proposed: R. Q. Yang (1995) Design Improvements: Meyer & Vurgaftman (1996-1997)
1st Experimental Demo: U. Houston & Sandia (1997)
Further Development: ARL, Maxion, JPL, U. Oklahoma, U. Würzburg
Disadvantage:
Spatially indirect (but good good gain for thin QWs)
3D Density-of-States
Advantages:
(1) Excellent electrical confinement
(2) Access to much longer 

## Slide 49
Full layered structure
Active ICL stages surrounded by separate confinement & optical cladding layers, each separated by transition regions
Full structure: 7–8 mm thick & > 3000 layers (takes 7-8 hours to grow)
Lattice-Matching: Each region carefully strain-compensated to minimize dislocations
Yield: Surprisingly high – Most NRL ICL wafers produce high-quality lasers
n+-GaSb Buffer & Substrate
Transition
n-InAs/AlSb SL Clad ( 4.0 m)
Transition
GaSb SCL
Transition
Active ICL Stages
“W” QWs + Injectors
Transition
GaSb SCL
Transition
n-InAs/AlSb SL Clad ( 2 m)
Transition
n+-InAs Cap (0.02m)
5x
900x
Notes: 49

## Slide 50
Figures of merit
Vurgaftman et al., Nature Com. 2, 585 (2011)
Single mode
High power
Revue: Vurgaftman et al., NJP 11, 125015 (2009), Meyer et al., Photonics West 2013
Notes: 50