## Slide 1: A wide introduction to IR imaging detectors Olivier Gravrand CEA-LETI Grenoble
CIRS Cassini detector (LW LETI)
TP2 detector (MW LETI)
olivier.gravrand@cea.fr
Notes: Apollinaire: « il est grand temps de rallumer les étoiles »

## Slide 2: Outline
General introduction about IR detection
FOM for IR detection/imaging
Tailoring the photocurrent
Understanding the dark currents
Impact ionization for APDs
Focus1: Ultra high performances for very low fluxes
Focus2: High operating temperature
Conclusion

## Slide 3: The EM spectrum from the IR point of view
0.1
1
10
100
1000
E (eV)
10
1
0.1
0.01
0.001
Visible
UV
NIR
SWIR
MWIR
LWIR
VLWIR
Tatmosphere
0
100%
IR  small energies(< eV)
Interest
  Corresp to molecular vibrations
  BB passive detection…
  Atmospheric windows…
  …
Lambda
(µm)
1000
100
10
1
f (THz)
kT@300K=26meV
1e4
1e3
100
10
TBB (K)
300K
2000K
600K
BB Luminance
Notes: kT@300K=26meV
kT@77K~9meV

## Slide 4: Principle of IR detection: general concepts
Read out circuit
SIGNAL
Thermal insulation
Thermometer
Read out circuit
SIGNAL
Quantum detector
=
« cooled » detector
Conversion   e-
IR
Absorption
IR
Thermal detector
=
Uncooled detector
Signal=Current  photon flux
Signal=DT  optical power

## Slide 5:  Quantum detectors
PC = Photoconductor
Conductivity measnt under
  Low cost
  Large bias
  Strong current
  Noise
  mainly 1D (1st Gen)
PV = Photovoltaic
Direct measnt of the current
  low current = low noise
  Fast response
  2D arrays possible
  Complex process (costy)

## Slide 6: ≠ Absorption Mechanisms  ≠ Spectral Shapes
l
Ej
E
Absorption
Valence band
Conduction band
Eg
Eg
lc
l
Ej
E
Absorption
Valence band
Conduction band
Eo
Eo
lc
l
Ej
E
Absorption
Eo
lo
Eo
Intrinsic material
Extrinsic material
Quantum well

## Slide 7: The Super-lattice (SL) material
Sullivan 2005,
SPIE5783 p151
Yu, « fondamental of semiconductors », Springer
2 ways to understand this synthetic material
Modulation of the cristal potential in one axis to fold the Brillouin zone, creating minibands
Coupling of a large number of Qwells by getting them closer in ordre to form the minibands
/!\ No selection rules for the optical absorption (≠ QWIP)
Aifer 2005, SPIE5783 112

## Slide 8: Bulk SC materials for IR detection
SWIR
LWIR
MWIR
-0.3
0.0
0.3
0.6
0.9
1.2
1.5
1.8
2.1
2.4
2.7
3.0
5.4
5.6
5.8
6.0
6.2
6.6
6.4
0.4
0.8
1
1.5
2
3
5
8
12
Bande interdite (eV)
Paramètre de maille (Å)
Longueur d’onde de coupure (µm)
Si
Ge
GaAs
InAs
InP
AlAs
AlSb
GaSb
ZnTe
CdTe
HgTe
InSb
Visible
HgCdTe SWIR
HgCdTe MWIR
HgCdTe LWIR
>VLWIR
O. Gravrand, JEM 36(8), p981, 2007
Notes: On peut examiner ces différentes bandes spectrales en regard des matériaux semiconducteurs absorbants bulk
Commentaire SL2 InAs-GaSb: matériaux synthétiques avec alternances de couches grand gap pour générer des minibandes autour d’un petit gap…
…
Pendant mon travail au leti, j’ai eu la chance de pouvoir travailler sur la quasi-totalité des filières IR existantes
InGaAs, InSb, InAsSb, HgCdTe, SLS…

## Slide 9: Détection by integration
Detector
Quantum detector = photon-electron conversion  Quantum Efficiency
Detected quantity = Photon flux
 Poisson statistic for a given integration time  photocurrent shot noise with
optimum
Proximity electronics Additional read out noise
A good detector requires:
High in order no to loose incoming information
Low additional noise in order not to degrade this information
Field of view
W
Proximity electronics
Output signal
Optics
Scene
t
t
I
t
I

## Slide 10: Photocurrents in pn junctions
Collected photocurrent limited by minority carriers
  N side: holes h+
  P side: electrons e-
  Space charge region (SCR)
IR
IR
Planar structure
Mesa structure
Diffusion
BV
BC
EF
Vbi
N: ND
P: NA
SCR
Wzce

## Slide 11: Spectral QE for Diffusion extracted Narrow gap photodiode (ex MCT)
interconnect
ROIC
Without CZT substrate:
  Flat QE on a very wide spectral band
  From IR up to visible… and UV!
O. Gravrand, JEM 40(8) p. 1781, 2011
IR
MCT

## Slide 12: Spectral QE for Diffusion extracted Narrow gap photodiode (ex MCT)
 without AR 
single layer AR (ex ZnS)
Multilayer AR …
Layer thickness
  eMCT = 8µm
  eMCT = 1µm
interconnect
ROIC
MCT
IR
Electrical collection efficiency
  Ld = 20µm (eMCT=20µm)
  Ld = 6µm
Pixel optical area  pixel fill-factor = QE net loss
Projet Vermisel 2005
O Gravrand QSIP 2012
Beer Lamber
Diffusion
PhD J. Berthoz

## Slide 13: Pixel level filtering
Incident interface metaljic filters (IDEP 2012)
Diode contact nano texturation in order to tailor the spectral shape
and optimise dark current
PhD M. Duperron
2013
PhD E. Lesmanne

## Slide 14: Outline
General introduction about IR detection
FOM for IR detection/imaging
Tailoring the photocurrent
Understanding the dark currents
Impact ionization for APDs
Focus1: Ultra high performances for very low fluxes
Focus2: High operating temperature
Conclusion

## Slide 15: PN junction dark currents
N and P sides : Auger et SRH generation  diffusion limit
SCR:
  No Auger in SCR
  SRH in SCR= GR
Surface currents
  Local degradation
BV
BC
ZCE
N: ND
P: NA
ER
EV
EF
VHg MCT specificity
SRH on EV
PVHg
CMT
In Bump
NIn
In Bump
VHg
Vhg
VHg
VHg
VHg
VHg
VHg
In
In
In
In
In
In
In
MCT N/P :VHg
MCT P/N :In
SCR
Thermal behaviour
Is dominated by

## Slide 16: ≠ recombination mechanisms
k
E
 Mechanisms limiting mino lifetime:
hn
Radiative
Schockley-Read-Hall
BC
BV
Heavy h+
BV
Light h+
Auger 1
Limiting N type
i
f
f
Auger 7
Limiting P type
i
i
f
1 h+light + 1 e-
 2 h+heavy
2 e-
 1 h+heavy+1 e-

## Slide 17: Mino carrier Lifetime battlefield…
Chart: 
| 6E+16 | 1.6E+16
MCTp x=0.23 (Kinch 05) | 5e-08 | 4.4e-07
Chart: 
| 8.0835E+17 | 4.4552E+17 | 1.9849E+17 | 1.094E+17 | 7.5657E+16 | 5.307E+16 | 3.3232E+16
Auger théo | 2.8523e-09 | 5.0041e-09 | 8.6238e-09 | 1.4102e-08 | 2.0038e-08 | 3.055e-08 | 6.1706e-08
MCTp x=0.23 (Kinch 05) | 5e-08 | 4.4e-07
Chart: 
| 1.0523E+17 | 1.8948E+17 | 2.3186E+17 | 3.569E+17 | 5.1736E+17 | 6.5083E+17 | 8.2783E+17 | 1.5979E+16 | 1.2971E+16 | 1.1789E+16 | 1.0556E+16 | 8491300000000000 | 8223900000000000 | 7136500000000000 | 6616600000000000 | 7448100000000000 | 5992600000000000
Exp | 4.3197e-09 | 4.3348e-09 | 3.7942e-09 | 2.504e-09 | 1.7276e-09 | 1.2833e-09 | 8.9805e-10 | 5.673e-09 | 1.0452e-08 | 4.2006e-09 | 7.5157e-09 | 6.9659e-09 | 5.4031e-09 | 5.9045e-09 | 4.7175e-09 | 8.0816e-09 | 6.9515e-09
Auger théo | 2.8523e-09 | 5.0041e-09 | 8.6238e-09 | 1.4102e-08 | 2.0038e-08 | 3.055e-08 | 6.1706e-08
MCTp x=0.23 (Kinch 05) | 5e-08 | 4.4e-07
SL2 : tSRH=6 ns
T2SL
expt
T2SL
theo
LW, T=77K
Doping (cm-3)
t (s)
Kinch 05, JEM 34(6) p880 (2005)
Pellegrino 09, SPIE7298 67
LETI MCTT:In
LETI MCT:VHg
Lin 14, JEM43(9) p3184
Youngdale94, APL64(23) p3160
Rhem 14, SPIE9070 0T
t Auger7
MCT p
t Auger1
MCT n
CMT : tSRH>2-20 µs
t VHg
MCT p
35 ns
Ga free SL2 450 ns
PhD B. Delacourt
InAs/GaSb
InAs/GaInSb
InAs/InAsSb:

## Slide 18: MCT n/p VHg = std process @ Sofradir
G.L.Hansen, JAP54 (1983) p1639
Gravrand, JEM, 36(8), p981, (2007)
Hg vacancy (VHg) = P type dopant in MCT (control by annealing T°)
Short lifetime =
  Low diffusion length
  High dark current
Depletion ?
/ 0.5µm
Diffusion
O Gravrand, To be published
JEM 2016

## Slide 19: Switch to extrinsic N:In doping
O. Gravrand, SPIE 636118–10 (2006)
O. Gravrand, JEM 38(8), (2009)
T. Chuh, SPIE 5563 p19 (2004).
W. Tennant, JEM, 37(9), p1406 (2008)
N. Baier, SPIE87042P (2013)
O. Gravrand, JEM 2016, to be published
P:VHg doping
   Short lifetime (~ns), SRH VHg recombinaison
Extrinsic N:In doping
  Longer lifetime (~µs) Auger1
  Larger  higher
 Gain close to x100 on
T=78K
Notes: Coupure psn jusqu’à 20µm à 50K
? A refaire avec les points psn en orange?

## Slide 20: Dark current optimisation for diffusion extracted extrinsic photodiode
t (s)
Nd (cm-3)
MCT p/n
T=150K
lc=5µm
tSRH=20µs
Auger1:
: Beattie & Landsberg (FF=0.47) in extr. regime
SRH
T2SL
t = 10xtAugerMCT
tSRH=80ns
O. Gravrand, “Challenges for ultimate HOT quantum IR detectors,”
SPIE 8631, 2013
Schockley-Read-Hall
Auger 1
Limite le type N
f
i
i
2 e- +1 h+lourd
 1 e-
PhD B. Delacourt

## Slide 21: Dark current optimisation for diffusion extracted extrinsic photodiode
t Nd (s.cm-3)
Nd (cm-3)
MCT p/n
T=150K
lc=5µm
tSRH=20µs
T2SL
t = 10xtAugerMCT
tSRH=80ns
Nd~1e15cm-3
Rule07
Nd~6e16cm-3
Caution
High doping=
lower Ldiff
lower QE ?
Need a highly absorbing material to minimize diffusion volume
Material intrinsic property
Lower ni by design for T2SL?
O. Gravrand, W. Hassis, and J. Rothman, “Challenges for ultimate HOT quantum IR detectors,”
SPIE, vol. 8631, Invited Paper, p. 50, 2013

## Slide 22: From single diode to focal plane array
Ideally we want all pixels identicals!
  TV/4 = 320x256 = 81 920 px
  TV = 640x512 = 327 680 px
Nice Gaussian distributions?
  Mean performances, PRNU, DCNU…
  Dispersion, operability = 1- defectuosity
O. Gravrand, JEM 38(8), (2009)
n/p VHg
n/p Ext
[nA]
Notes: Faire une bonne diode c’est bien…Faire un plan focal, c’est plus dur…

## Slide 23: Impact ionisation for MCT APDs
BV
BC
N: ND
P: NA
ER
EF
electron
hole
BV
BC
PVHg
CMT
In Bump
PVHg
CMT
In Bump
PhD G. Perrais
(2009)
G. Perrais,JEM36(8) p963(2007)
/!\ tunnel current limitation
Single e- multiplication (no hole Xcation)
quasi deterministic Pionisation
Low additional noise
before amplification
with gain
XS noise
APD = Avalanche Photodiode
Photocurrent pre-amplification in the jonction
Overcome read out electronic noise
  Impact Ionisation
  1e-  2e- + 1h+
  
  (Auger7)-1

## Slide 24: What is interesting in this APD gain?
Top ____ sRN=50e
Shot limit sN²=<N>
SFD 2011 sRN=9e
APD MCT sRN=50e M=30 F=1
APD Si and/or 3-5
sRN=50e M=30 F=2
M=30 F=5
Photon nb = <N>
F=RSBin/RSBout
RO noise= 50e
9e
Input equ.
RO noise
= 50e /30
Alternative: Current pre-amplification with avalanche gain before RO in order to deconstrain proximity electronics design
100e
APD gain + F~1 for MCT allows to extend the detection range at low photon nb
wo Gain, RO noise
Std -------- sRN=100e
 in²=2qI
Sténopé
Notes: Limite absolue de SNR : pour une diode parfaite en N²/s où s=N.
Ajoute le bruit de lecture du CL : plus le flux est faible, moins on fait ressortir le signal. Ex cas sténopé.
Cas des APD à F>1  dans des applications fort flux, à cause de l’excès de bruit, on perd de l’information ! Tous les APD ne sont pas bons pour toutes les applications !

## Slide 25: Outline
General introduction about IR detection
FOM for IR detection/imaging
Tailoring the photocurrent
Understanding the dark currents
Impact ionization for APDs
Focus1: Ultra high performances for very low fluxes
Focus2: High operating temperature
Conclusion

## Slide 26: Very high performance issue
Notes: Graphique Arhenius

## Slide 27: Very high performance issue
CZT substrate
N type
absorbing layer
P type
cap
Ec
EF
Ev
PN junction

## Slide 28: Very high performance issue

## Slide 29: Very high performance issue
CZT substrate
N type
absorbing layer
P type
cap
Ec
EF
Ev
PN junction
SCR currents
Surface currents

## Slide 30: Very high performance issue
Material and process quality improvement
Burried junction risk
Barrier formation on the VB
EB<kT : QE loss at low T°
(thermionic curent at high T°)
CZT
N type
absorbing layer
P
Ec
EF
Ev
Jonction PN
X
SCR currents
Surface currents
Heterostructure Photodiode

## Slide 31: Very high performance issue

## Slide 32: NIR high performance issue
Diffusion VHg
GR
56e/s/px30µm
Diffusion VHg
GR
56e/s/px30µm
LETI-SAp 2012
2.5µm p/n planar MBE/CZT
NIRLFSA phase 1
LETI-SAp 2012
2,03µm p/n planar MBE/CZT
NIRLFSA phase 1
LETI-SAp 2012
1.96µm n/p planar LPE/CZT
NIRLFSA phase 1
SAp 2015
2.08µm p/n planar LPE/CZT
NIRLFSA phase 3
SAp 2015
2.12µm p/n planar MBE/CZT
NIRLFSA phase 3
SAp 2015
2.08µm p/n planar LPE/CZT
NIRLFSA phase 3
SAp 2015
2.12µm p/n planar MBE/CZT
NIRLFSA phase 3
LETI 2014
3µm n/p APD LPE/CZT
M=1
ROIC1 SFD p15 TV/2
ROIC2 SFD p15 TV
ROIC2 CTIA
p30TV/2
M=7,5 / V=6.3V
0.1e/s/px
0.04e/s @ 45K
1e/s/px
Jdark (A/cm²)
Temperature (K)
lc=3µm @ 80K
Ongoing caracterisation…
APD FPA / SFD ROIC
lc=2.5µm @ 78K
VRST=800mV
Tint=5s

## Slide 33: Outline
General introduction about IR detection
FOM for IR detection/imaging
Tailoring the photocurrent
Understanding the dark currents
Impact ionization for APDs
Focus1: Ultra high performances for very low fluxes
Focus2: High operating temperature
Conclusion

## Slide 34: HOT issue
HOT = High Operating Temperature
SWAP: Size Weight And Power (Price)
Cryo Machines
  Cooler engine lifetime
  Consumption
Expected as a (very?) large market for IR detectors…
Important commercial issue
Large technical issues:
  Dark current reduction
  Defectuosity management
  Very low pixel pitches expected…

## Slide 35: HOT dark current issue
167
250
125
100
83
71
T (K)
1000/T (K-1)
Jdark (A/cm²)
InSb SCD [Shtrichman12]
tSCR=150ns
tSRH=300ns
Rule07  MCT
lc=5.3µm@80K
Epi-InSb SCD [Shtrichman12]
Rule07
lc=4.1µm@150K
F#/2 300K lc=5.3µm
F#/2 300K lc=4.1µm
150K
180K
80K
nBn, 0.6V, InAsSb SCD
[Klipstein11]
nBn, 1.2V
Shtrichman 2012, SPIE83532Y
Klipstein 2011, SPIE80122R
GR
InAsSb
AlAsSb
NBN barrier devices
GR
Notes: Tblip red 201K – blue 195K

## Slide 36: The real FOM is the noise…
MW (lc=5.53µ@77K) n/p VHg (var size)
in (A/√Hz) [10;30Hz]
Idark (A)
Shot noise
in = √2qI
Bruit 1/f
in  I
All photodiodes have intrinsic 1/f noise sources
  @ low currents, shot noise usually dominates
  @ high currents, 1/f appears…
@ higer T°, shot noise usually don’t dominates any more!
Low T°
= low current
High T°
= high current

## Slide 37: For the FPA point of view
Jdark (A/cm²)
in² (A²/Hz/cm)
Shot noise
N:In
P:VHg
  Some px are more affected by 1/f than others
  Noise operability degradation (distribution tails )
  Limitation before the shot – 1/f knee T°
   Material and process improvement to minimize 1/f noise sources
PhD A. Brunner

## Slide 38: XS noise histogram examples…
Population
Population Cumulée
Probabilité Cumulée
Cumulated probability (gausso-arithmetic scale)
MCT p/n MW TV p15µ 130K Tint = 4ms / Cint = 480fF BB20°C
InSb TV/4 p30µ 80K Tint = 1.4ms / Cint = 455fF BB25°C

## Slide 39: Conclusions
Science :
  ROIC glow is limiting ultimate performances
  APDs allows to push the detection limits to very low photon nb
  More pixels, larger overall area  very large formats
HOT MW:
  Today structures (150K)
    Improve defectivity improving material and process quality
    Blue or red MW ?, MCT vs InAsSb ?
  Up coming structures (>150K)
    Decrease the dark current below rule07
    Change doping to be limited by Auger7 instead of Auger1?
    Fully depleted PiN diodes (very high SRH required >ms)
    Confinement structures to decrease Idark generation volume
  2k x 2k 15µm pitch = 3 cm
  4k x 4k 10µm pitch = 4cm
2kx2k 10µm pitch FPA @ LETI (mockup)

## Slide 40: Real imaging of a Valence Band….
Barrette Timbre Poste MW (LETI)
Valence

## Slide 41: acknowledgments DEFIR : laboratoire commu) LETI-Sofradir DGA : Direction générale de l’armement ESA: European space agency CNES: Centre national d’études spatiales FOCUS: IR detection for science (Labex)

## Slide 42: Thanks to all others…
Mega pixel MW FPA 10µm pitch MCT LETI